## Slide 1: The role of metal-oxide grain boundaries for applications in photovoltaics and spintronics
Keith McKenna
Department of Physics, University of York
Notes: 40 + 5

## Slide 2: McKenna Materials Modelling group
Structure and properties of nanostructured materials underpinning applications in areas such as electronics, energy and catalysis
Semiconductor electronics
Spintronics
Solar cells
Catalysis
Claudio Padilha (PDRA)
John Carey (PDRA)
Razak Elmaslmane (PhD)
James Quirk (PhD)
Jonathan Bean (PhD)
Steven Hung (PhD)
Adam Kerrigan (PhD)
Steven Hung (PhD)

## Slide 3: Introduction
Metal-oxides ubiquitous in nature and applications

## Slide 4
Extended defects in oxides
  Most oxides are polycrystalline  grain boundaries
  Oxide films often contain dislocations (lattice mismatch, non-equilibrium growth)
  Modified structure and defect segregation affects many properties
Also affects electronic properties
  high-Tc superconductors, solar cells, electroceramics, ferroelectrics, magnetic oxides, conducting oxides, microwave dielectrics, photo-catalysts…
  Not well understood as difficult to probe electronic properties of buried extended defects directly
Misfit edge dislocation
A. P. Sutton and R. W. Balluffi, Interfaces in Crystalline Materials (Oxford University Press, 1995)
Grain boundary

## Slide 5: Outline
Methods
Grain boundary controlled electron mobility in TiO2
Antiphase boundary defects in Fe3O4
Grain boundaries in magnetoresistive tunnel junctions

## Slide 6
Methods

## Slide 7
Atomistic interatomic potentials
  For ionic materials shell model potentials are very accurate and efficient
  Electrostatic + short range + polarisability
  Parameterised against experimental properties
  Low computational cost → large complex systems and efficient screening
G. V. Lewis and C. R. A. Catlow, J. Phys. C 18, 1149 (1985)
Y
O2-
Mg2+

## Slide 8
  Solve many-electron problem to determine most stable structure
  Density functional theory good compromise between accuracy and computational cost
  Predict structure of materials in 3D (dependence on conditions)
  Predict corresponding properties (including those that are difficult to measure directly)
First principles theoretical modelling

## Slide 9: Modelling extended defects
Bicrystal approach
  Consider well defined interface between two oriented crystals
  Find stable atomic structure by minimising energy with respect to:
    Intergrain translation and dilation
    Addition/removal of ions at interface
  Mimics experimental bicrystal approach often used in transmission electron microscopy
  Screen structures at classical level then at DFT level
K. P. McKenna and A. L. Shluger, Nature Materials 7, 859-862 (2008)
H.-S. Lee et al., Ultramicroscopy 111, 1531 (2011)
SrTiO3

## Slide 10: Defect induced structure transformation
(310)[001] MgO grain boundary
  Experimental collaboration with Yuichi Ikuhara, Univ. of Tokyo
  High purity crystals of well defined orientation thermally bonded
  Transmission electron microscopy (HAADF and ABF scanning TEM and electron energy-loss spectroscopy)
  DFT based simulated contrast provides excellent agreement
  Ordered defect superstructure involving Ca, Ti and VMg
Ca
Ti
O
Z. Wang, M. Saito, K. P. McKenna et al, Nature 479, 380 (2011)

## Slide 11
Grain Boundary Controlled Electron Mobility in TiO2

## Slide 12: Electron diffusion in polycrystalline TiO2
TiO2 applications
  Li-ion battery anode
  Dye sensitised solar cells
  Photocatalysts
  Resistive switching memory
Often highly nanostructured
  Many interfaces between nanocrystals (grain boundaries)
  How do grain boundaries affect electron (hole) mobility?
  Can they trap charge?
J. A. Anta, Curr. Opin. Coll. & Inter. Sci. 17 124 (2012)
C. Anselmi et al, Phys. Chem. Chem. Phys. 14, 15963 (2012)

## Slide 13: What is known?
S. Yang et al, Phys. Rev. B. 87,125201 (2013)
Small e polarons in TiO2 (rutile)
  EPR studies indicates photoinduced small polaron formation (Ti3+)
  Temperature dependence: not simple exponential decay
  Fitting to general order kinetics obtain activation energy ~ 25 meV (hopping/ionisation into CB?)

## Slide 14
F. Cao et al, J. Phys. Chem. 100,17021 (1996)
Role of interfaces
  Measured photocurrent diffusion coefficients much less than expected for free electrons (e.g. 10-2 cm2s-1 for anatase)
  Trap sites (bulk, surface & interface) suggested to control transport
  Strong intensity (current density) dependence on e diffusion
  Challenging to probe directly
M. Yanagida, Effect of the Charge Collection Electrode on Electron Transport in Nanocrystalline TiO2, IWAMSN2012 (2012)
Photocurrent rise time (s)
Power (mW cm-2)
Various models of role of interfaces

## Slide 15: Grain boundary in rutile
D. J. Wallis et al., J. Am. Ceram. Soc. 80, 499 (1997)
Rutile (210)[001] TiO2 grain boundary
  Predicted structure in good agreement with TEM studies
  Variation in ion coordination, strain and electrostatic potential near GB
Predicted structure coloured according to electrostatic potential @ Ti sites
TEM image of rutile (210)[001] TiO2 GB
Bulk-like Ti site
Perturbed GB site

## Slide 16: Electron polaron trapping energies in TiO2
Electron trapping
  DFT+U approach to correct self-interaction error (UTi=4.2 eV)
  Total energy for electron trapped at all inequivalent Ti sites calculated
  Dilate O ions by 0.08 Å around a given Ti to create precursor for localisation
  Trapping energy Et (eV) defined with respect to bulk Ti site
  Strong correlation between trapping energy and electrostatic potential (slope = -1.1 +/- 0.1)
more stable than bulk
less stable than bulk

## Slide 17: e diffusion perpendicular to grain boundary
Two possible paths in z-direction:
Eact (max) ~ 0.46 eV
Eact (bulk) ~ 0.28 eV
Path a:
Path b:
Eact (max) ~ 0.46 eV
Eact (bulk) ~ 0.28 eV
High trapping energy of site a4 could lead to blocking of path a  low intergrain connectivity

## Slide 18
Electron transport simulation
Kinetic Monte Carlo approach
  Electron transfer described using Marcus/Mott/Holstein theory
  Electron-electron electrostatic interactions included
  Model electron injection, hopping (in all directions) and absorption
S. Wallace and K. P. McKenna, Adv. Mater. Inter. 1, 1400078 (2014)

## Slide 19
S. Wallace and K. P. McKenna, Adv. Mater. Inter. 1, 1400078 (2014)

## Slide 20
S. Wallace and K. P. McKenna, Adv. Mater. Inter. 1, 1400078 (2014)

## Slide 21
Effect of grain boundary on electron mobility
  Grain boundary introduces sites with higher and lower trapping energies (+0.2 eV / -0.4 eV)
  Very stable trapping sites hinder electron transport - increases e transit time many orders
  Trap filling effect at higher electron currents (seen experimentally)
  Can improve transport by removing interfaces, n-doping or higher photocurrents
S. Wallace and K. P. McKenna, Adv. Mater. Inter. 1, 1400078 (2014)

## Slide 22
Antiphase Boundary Defects in Fe3O4

## Slide 23
Magnetite Fe3O4
  Abundant mineral and oldest known magnetic material
  fcc oxygen lattice with interstitial Fe – tetrahedral (tet) and octahedral (oct)
  tet and oct Fe sites with magnetic moments aligned antiparallel - ferrimagnetic material
  Predicted to be half-metallic at room temperature
  100% spin polarisation at Fermi energy attractive for spintronics applications

## Slide 24
Antiphase boundary defects in Fe3O4
  Fe3O4 thin films and bulk crystals have numerous APB defects
  Magnetite crystals produced by annealing Fe2O3 have networks of APBs on {110} planes
  Antiferromagnetic coupling across APBs has been proposed to explain negative magnetoresistance
  But challenging to probe locally and no detailed models of atomic structure

## Slide 25
Prediction of (110) APB structure
  Consider APBs forming on (110) plane
  Systematic search over all possible interface structures (translations and terminations)
  Screen using classical interatomic potentials then full DFT optimisation
  Identify all possible APB structures with low formation energy:
K. P. McKenna, F. Hofer, D. Gilks, V. K. Lazarov, C. Chen, Z. Wang and Y. Ikuhara,
Nature Communications 5, 5740 (2014)

## Slide 26
Two possible APBs found:
  APB-I
    crystal translation (1/4)a[110]
    Ef= 102 mJ/m􏰂2 (very low)
    no net change in Fe coordination
  APB-II
    crystal translation (1/4)a[110]+(1/4)a[1-10]
    Ef= 954 mJ/m􏰂2
  Both APBs involve diamond and hexagonal structural units
  Both APBs AF coupled (due to Fe-O-Fe bonds close to 180 degrees)
K. P. McKenna, F. Hofer, D. Gilks, V. K. Lazarov, C. Chen, Z. Wang and Y. Ikuhara,
Nature Communications 5, 5740 (2014)
APB-I
APB-II

## Slide 27
Transmission electron microscopy
  HAADF-STEM imaging of (110) APBs in Fe3O4 with atomic resolution
  Images taken along the [1-10] and [1-11] directions􏰁
  Compared to simulated TEM images using DFT structures
  Clearly resolve hexagon diamond structural units
  No asymmetry suggesting APB-I model
K. P. McKenna, F. Hofer, D. Gilks, V. K. Lazarov, C. Chen, Z. Wang and Y. Ikuhara,
Nature Communications 5, 5740 (2014)

## Slide 28
Electronic properties of APB (AF ground state)
Spin polarization reverses direction across the APB plane, hence the transport of electrons between the domains in both spin states will be associated with substantial scattering
Away from APB bulk electronic structure recovered rapidly

## Slide 29
Explanation of high stability of (110) APB
  Diamond and hexagonal structural units are highly stable (not seen in cubic Fe3O4)
  Are they stable as a bulk phase?  Pmma phase
  DFT calculation indicates Pmma Fe3O4 is only 332 meV per formula unit less stable than the cubic
  Pmma phase is also ferrimagnetic and could be stablised by strain in nanostructures
K. P. McKenna, F. Hofer, D. Gilks, V. K. Lazarov, C. Chen, Z. Wang and Y. Ikuhara,
Nature Communications 5, 5740 (2014)

## Slide 30
Grain Boundaries in Magnetoresistive Tunnel Junctions

## Slide 31: Magnetoresistive tunnel junctions
Z. Wang, M. Saito, K. P. McKenna, S. Fukami, H. Sato, S. Ikeda, H. Ohno and Y. Ikuhara
Nano Letters 16, 1530 (2016)
CoFeB/MgO tunnel junctions
  Large change in resistance on application of magnetic field
  Due to spin-dependent tunnelling through thin MgO barrier
  Applications in hard disk read heads and STT-RAM
  MgO barrier is usually polycrystalline
  Effect on electronic properties?

## Slide 32
MTJs from Hideo Ohno’s group, Tohoku University, Japan (TMR> 600%):

## Slide 33
J. Bean et al, Sci. Rep. 7, 45594 (2017)

## Slide 34
J. Bean et al, Sci. Rep. 7, 45594 (2017)

## Slide 35
J. Bean et al, Sci. Rep. 7, 45594 (2017)

## Slide 36
Conclusions
  [001] tilt grain boundaries present in MgO layer of MTJ
  Local band gap reduced significantly at GBs (by up to 3 eV)
  Predict shunting of current through GBs and associated reduction of TMR
  GBs must be passivated to achieve highest TMR

## Slide 37: Summary
DFT investigation of defects
  Oxides find diverse applications where defects control performance
  Defects possess complex electronic, magnetic, optical and chemical properties
  Often challenging to probe by experiment alone
  Examples presented show how materials modelling can complement experiment and help understand defect properties and functionality

## Slide 38
Polarons
Intrinsic defects
Impurities
Surfaces
Grain boundaries
Dislocations

## Slide 39: Acknowledgements
People:
J. Bean, F. Hofer (Physics, York)
D. Gilks & V. K. Lazarov (Physics, York)
C. Chen, M. Saito & Y. Ikuhara (WPI-AIMR, Tohoku University & The University of Tokyo)
S. Fukami, H. Sato, S. Ikeda, H. Ohno (RIEC, Tohoku University)
Funding:
EPSRC Fellowship (EP/K003151)
EPSRC grants (EP/K03278X and EP/K013114)
Nuffield Foundation and Institute of Physics
COST Action CM1104
Computational time:
UK Materials Chemistry Consortium (EPSRC grants EP/F067496 & EP/L000202)

## Slide 42
Interdiffusion in Magnetoresistive Tunnel Junctions

## Slide 43: Magnetoresistive tunnel junctions
Z. Wang, M. Saito, K. P. McKenna, S. Fukami, H. Sato, S. Ikeda, H. Ohno and Y. Ikuhara
Nano Letters 16, 1530 (2016)
CoFeB/MgO tunnel junctions
  Large change in resistance on application of magnetic field
  Due to spin-dependent tunnelling through thin MgO barrier
  Applications in hard disk read heads and STT-RAM
  Interaction of Co, Fe and B with MgO – is there any interdiffusion?
  Effect on electronic properties?

## Slide 44
DFT investigation of defects in MgO
  DFT PAW (VASP), PBE functional
  Ecut=400 eV, k=9x9x9
  Consider B, Co and Fe incorporation into interstitial, anion and cation sites of MgO and also Ta
  Consider incorporation of ions in all possible charge states
  Formation energies calculated:
  Co20Fe60B20 used to define B, Fe and Co chemical potential
Chemical potential – determined by electrode and O partial pressure
Fermi energy – determined by electrode band offset/applied voltage

## Slide 45: B defect formation energies
B most favourable in fcc Ta interstitial site
If oxygen poor then B incorporation in MgO difficult
If oxygen rich can incorporate as 3+ or 1+ ion in cation site
Z. Wang, M. Saito, K. P. McKenna, S. Fukami, H. Sato, S. Ikeda, H. Ohno and Y. Ikuhara
Nano Letters 16, 1530 (2016)

## Slide 46: EELS mapping
As grown
Annealed
Boron diffuses into Ta. No evidence for B in MgO.
Z. Wang, M. Saito, K. P. McKenna, S. Fukami, H. Sato, S. Ikeda, H. Ohno and Y. Ikuhara
Nano Letters 16, 1530 (2016)

## Slide 49
Additional slides

## Slide 50: A complex problem
  Interfaces between anatase & rutile nanocrystals
  Role of surfaces as trapping sites (including steps, corners, etc)
  Role of dye molecules
  Role of electrolyte
  Hydroxyls, impurities and intrinsic defects
  Mechanisms of e transport
  Recombination effects
B. Buesser, A.J. Gröhn and S.E. Pratsinis, Sintering Rate and Mechanism of TiO2 Nanoparticles by Molecular Dynamics, AIChE Proceedings (2011)

## Slide 51: Modelling electron trapping
Density functional theory
  VASP code: plane wave basis and PAW method
  PBE functional
  Ecut=500 eV, k=6x6x9 for rutile conventional cell
  Force tolerance 0.01 eV/Å
  Rutile TiO2 lattice constant within 2% of experiment (a=4.67 Å, c=3.03 Å)
  DFT+U correct self-interaction error for trapped electron
  Here use UTi=4.2 eV (fitted to spectroscopic properties of oxygen vacancies)
D. Muñoz Ramo, et al, Phys. Rev. Lett. 99, 155504 (2007)
N. A. Deskins and M. Dupuis, Phys. Rev. B 75, 195212 (2007)
B. J. Morgan and G. W. Watson, Surf. Sci. 601 5034 (2007)
Rutile TiO2
Electron polaron trapped on Ti ion

## Slide 52: Electron polaron trapping energies in TiO2
Electron trapping
  Total energy for electron trapped at all inequivalent Ti sites calculated
  Dilate O ions by 0.08 Å around a given Ti to create precursor for localisation
  Trapping energy Et (eV) defined with respect to bulk Ti site
  Strong correlation between trapping energy and electrostatic potential (slope = -1.1 +/- 0.1)
more stable than bulk
less stable than bulk

## Slide 53: Parallel to grain boundary (y-direction)
Eact=0.28 eV
a1
a1
a1
a1
Bulk diffusion in (001) direction Eact=0.23 eV (i.e. electrons less mobile along dislocation line)

## Slide 54: Parallel to grain boundary (x-direction)
Eact(max)=0.58 eV

## Slide 55
Marcus theory
  Consider charge transfer between 2 species in a polarisable medium (e.g. He in water)
  Two isoenergetic equilibrium configurations
  Identify collective coordinate for polarisation of medium, Q
He0
He+
Electron transfer rate is given by
Modelling electron transfer

## Slide 56
Electron hopping rate
  Adiabatic electron transfer with rate:
  Activation energies from DFT calculations (Marcus-like model):
  Parameters: el = 1,  = 24 THz, Eact (bulk)= 0.3 eV, Hab = 0.2 eV, kBT = 0.026 eV
  Qualitative trends not affected by parameters but absolute currents are
N. A Deskins and M. Dupuis, Phys. Rev. B 75, 195212 (2007)

## Slide 57
Electron-electron interactions
  Consider interaction between two electrons in bulk

## Slide 58: Calculation of Hab and λ
Multi-reference wavefunction methods
  Hab accurate but computationally expensive
  Convergence with respect to atomic basis set
  Limited to small molecular systems
  λ requires forces (prohibitively expensive)
Density functional theory
  Large systems (>300 atoms) and forces
  Self-interaction error
    poor description of charge localised states
    even for hybrid functionals with non-local exchange
  Finite size effects (Hab and λ) for periodic boundary conditions
Hole transfer in C2H4-(CH2O)n-C2H4
TiN/HfO2/TiN tunnel junction
F. Plasser and H. Lischka, J. Chem. Phys. 134, 034309 (2011)
Notes: Ethylene-formaldehyde-Ethylene

## Slide 59
Constrained density functional theory
  Constraint to enforce localisation of electron on donor or acceptor
  Construct Hamiltonian in this diabatic (charge localised basis)  Hab given by off-diagonal elements
D----------A
D----------A
final state
initial state
Q. Wu and T. van Voorhis, Phys. Rev. A 72, 024502 (2005)
H Oberhofer, JB, J. Chem. Phys. 133, 244105 (2010)
Electron transfer in (He-He)+
  Good agreement with multi-reference methods for molecular systems
  Implemented in CPMD code
    periodic plane wave basis
    Troullier-Martins or Goedecker-Hutter pseudopotentials
    GGA and hybrid functionals

## Slide 60
Landau-Zener theory
(Hab)
Transition state theory
(Hab, λ)
Initial
Final
TS
Marcus theory

## Slide 61: Cancelation of nonlinearity (CON) method
Predicting polaron formation
  Often parameters (U or HF%) fitted to experimental properties (e.g. band gap)
  Does not guarantee self-interaction is eliminated therefore cannot predict polaron formation
  An exact functional should satisfy Janak’s theorm:
    Linear dependence of energy on fractional occupation
    LDA/GGA is convex (delocalised), HF is concave (overlocalises)
  An exact functional should satisfy the DFT-Koopmans’ condition
M. Cococcioni & S. de Gironcoli, Phys. Rev. B 71, 035105 (2005)
S. Lany and A. Zunger, Phys. Rev. B 80, 085202 (2009)
VB
CB
add electron (E+/0)
ei
N
E
Exact
N+1
N-1
DFT
HF

## Slide 62: Hole trapping in m-HfO2/ZrO2
Perfect lattice properties
  Calculation details
    VASP, PBE, 400 eV, k=83
    Crystal structure within 1% of experiment
    m-HfO2 and m-ZrO2 very similar (focus on hafnia in the following)
  Monoclinic structure
    7C cations
    3/4C anions arranged into 2D layers
  Electrostatic (Madelung) potential
    potential is 0.36 V higher on 3C oxygen ions than 4C oxygen ions
[100]
[001]
3C
4C
3C
4C
4C
K. McKenna et al, Phys. Rev. Lett. 108, 116404 (2012)

## Slide 63
Electronic properties
  Projected DOS shows top of valence band has O3C character
    splitting between 3C and 4C correlates with electrostatic potential
  Hole introduced vertically is delocalised over 2D 3C-O planes
  Dispersion in [100] is small
  Therefore, for holes m-HfO2 is a layered 2D material
  If a polaron forms, does it only form in the 3C-O plane?
3C
4C
3C
4C
4C

## Slide 64
Self-consistent determination of the hole potential
λhs
E – EVBM (eV)
E+/0
ei
4C O
E+/0
ei
3C O
All polaron calculations use 324 atom unit cell and energies corrected for finite-size effects (image-charge and potential alignment )
λhs=3.8 eV

## Slide 65
Properties of polarons in m-HfO2
  Spin density > 70% localised on oxygen (O-)
  Charge transition level lower on 4C O by ~ 0.3 eV (electrostatic potential difference)
  Trapping energy (stability relative to delocalized hole in valence band)
    Et (3C) = 0.18 eV
    Et (4C) = -0.31 eV [metastable]
  Therefore, hole polarons in HfO2 are confined within 2D layers

## Slide 66
Why is the 4C O ion less stable?
  Four terms: kinetic energy, polarisation, strain, electrostatic potential
  Kinetic energy and polarisation terms similar for both 4C and 3C
  Difference is due to strain (Es) and electrostatic potential

## Slide 67: Barrier to hole self-trapping
[001]
[100]
[001]
[010]
  20 meV fluctuation sufficient for 2D localisation
  40 meV barrier to self-trapping

## Slide 68
Polaron mobility
  Highly anisotropic activation energy
    within 3C planes 0.14 eV
    perpendicular to 3C planes > 0.60 eV
  Hopping mechanism
    thermal trapping energy (0.18 eV) is comparable to activation energy
    ionisation/re-trapping (Frenkel-Poole emission) seems to be the relevant transport mechanism
  Experimental high temperature conductivity measurements
    p-type (hole ionisation form cation vacancies)
    activation energy 0.2 eV
[100]
[001]
N. M. Tallan, W. C. Tripp, and R.W. Vest, J. Am. Ceram. Soc. 50, 279 (1967)